Heading, name, adddress, telephone number and official details of the applicator providing this certificate of fireproofing

CERTIFICATE OF FIREPROOFING N° 020 /2014

GTFI Member n° 0800

The undersigned applicator, a member of the French technical fire prevention group« Groupement Technique Français contre l'incendie » (GTFI) certifies that the materials and/or elements comprising the subject of this document have been fireproofed in conformity with the legislation and rules in force, using the products referenced by the GTFI in compliance with the technical conditions imposed by the manufacturer consistent with the rules the profession. The applicator has completed this certificate under its own responsiblity. Testing carried out by the security commissions does not free the applicator from its personal responsiblilities.

Materials and or elements treated

Nature of the material

Fabrics x wood various : cellulose fiber_______________________

Exact description : Cardboard unit (card module)__________________________

Developed surface treated ; XXXXX m2 ____ or number(s) of units treated XXX units_________

Marking : NO ____________________________________________________________________

Quantity/(ies) of fireproofing product(s) used : 150g/m2 (concentration of chemicals)
Mode of treatment soaking (daubing?)« Foulardage » Spraying Others

Self-administered testing

Equipment : Bunsen burner (control equipment)
Results of self-administrered testing (*) No propagation or flame persistence.
(*)A fire classification of the finished material would require tests carried out by an approved laboratory on request of the customer.

Comments :_______________________________________________________________
Maintenance advice________________________________________________________

Products or procedures used :

Trade name of the fireproofing product or products : EUROFIBRE …. Batch N° 1114/AFT
Manufacturer : SARL ALFA FLOR
Official record n° 18305-14 …......................... Official Laboratories : Héraklès ; Safran ; SNPE
Materials (Support) cellulose fibers …................
Fire classification indicated on the official record M1 ; (B1) ; A2, s1d1
Durability of the treatment : No time limit ….................

Further information :
Date and place of procedure : Workshops
11/02/2015
Name and address of customer : NIKITA PUBLICITE 82000 Montauban, salon d'exposition Berlin

Invoice number : FA15XXXX

In PARIS
NKT

On 11 February 2015